## Slide 1: Single-sheet inorganic colloidal dispersions are common and easily prepared
Ion exchange: (fixed charge density)
  smectite clays Nax+yAl2-yMgySi4-xAlxO10(OH)2
  layered double hydroxides Mg3Al(OH)8Cl
  layered oxides CsxTi2-x/4x/4O4
  metal phosphorous sulfides K0.4Mn0.80.2PS3
Redox reaction: (variable charge density)
  metal dichalocogenides LixMoS2
  layered oxides LixCoO2 , NaxMoO3

## Slide 2: Intercalation/exfoliation
Graphite exfoliation
Layered chalcogenide exfoliation
Can we make colloidal [graphenium]+ or [graphide]- sheets

## Slide 3: …if you have the correct sheet charge density and an appropriate polar solvent
Intercalation compound Swollen Colloidal
No solvation solvent in galleries solvated ions/sheets
DHL > DHsolv
DHsolv > DHL
higher surface charge density
lower surface charge density

## Slide 4: Graphite structure
C-C in-plane = 1.42 Å
Usually (AB)n hexgonal stacking
Interlayer distance
= 3.354 Å
http://www.ccs.uky.edu/~ernst/
A
B
A
Graphite is a semi-metal, chemically stable, light, strong

## Slide 5: Graphite Lithiation
Graphite lithiation: approx 0.2-0.3 V vs Li+/Li
Theoretical capacity:
Li metal > 1000 mAh/g
C6Li 370
Actual C6Li formation: 320 – 340 mAh/g reversible;
20 – 40 irreversible
Expands about
10% along z

## Slide 6: Li arrangement in C6Li
Theoretical capacity:
Li metal > 1000 mAh/g
C6Li 370
Typical C6Li formation: 320 – 340 reversible;
20 – 40 irreversible
Li+ occupies hexagon centers of non-adjacent hexagons

## Slide 7: GIC’s
Reduction M+Cx-
Group 1 except Na
Oxidation Cx+An-
F, Br3-, O (OH)
  BF4-, P  BiF6- , GeF62- to PbF62-, MoF6-, NiF62-, TaF6-, Re  PtF6-
  SO4-, NO3-, ClO4-, IO3-, VO43-, CrO42-
  AlCl4-, GaCl4-,FeCl4-, ZrCl6-,TaCl6-

## Slide 8: Staging and dimensions
Ic = di + (n - 1) (3.354 Å)
For fluoro, oxometallates di ≈ 8 A,
for chlorometallates di ≈ 9-10 A

## Slide 9: Graphite oxidation potentials
H2O oxidation potential vs Hammett acidity
Colored regions show the electrochemical potential for GIC stages.
49% hydrofluoric acid
All GICs are unstable in ambient atmosphere , they oxidize H2O

## Slide 10: New syntheses: chemical method
N
S
O
O
CF3
S
O
O
F3C
..
Cx + K2MnF6 + LiN(SO2CF3)2 CxN(SO2CF3)2 + K2LiMnF6
oxidant anion source GIC
1,2
1. 48% hydrofluoric acid, ambient conditions
2. hexane, air dry
Oxidant and anion source are separate and changeable. Surprising stability in 50% aqueous acid.

## Slide 11: CxN(SO2CF3)2 chem prepn

## Slide 12: New syntheses: N(SO2CF3)2 orientation
F
F
F
F

## Slide 13: Increasing F anion co-intercalate with reaction time
CxN(SO2CF3)2· dF
Katinonkul, Lerner
Carbon (2007)

## Slide 14: New syntheses: imide intercalates
Anion mw di / nm
1. N(SO2CF3)2 280 0.81
2. N(SO2C2F5)2 380 0.82
3. N(SO2CF3)(SO2C4F9) 430 0.83
1
2
3

## Slide 15: CxN(SO2CF3)2 echem prepn
2  1
3  2

## Slide 16: CxN(SO2CF3)2 - echem prepn
CxPFOS
CxN(SO2CF3)2

## Slide 17: Imide (NR2-) intercalates
Anion MW di / Å
N(SO2CF3)2 280 8.1
N(SO2C2F5)2 380 8.2
N(SO2CF3) 430 8.3
(SO2C4F9)

## Slide 18: CxPFOS - preparation
Cx+ K2Mn(IV)F6 + KSO3C8F17
 CxSO3C8F17 + K3Mn(III)F6
(CxPFOS)
Solvent = aqueous HF
3.35 A

## Slide 19: CxPFOS intercalate structure
Anions self-assemble as bilayers within graphite galleries

## Slide 20: New syntheses: CxSO3C8F17
Domains are 10-20 sheets along stacking direction

## Slide 21: Borate chelate GIC’s
1.12
0.78 nm
CxB(O2C2O(CF3)2)2
Stage 2
1.13
0.85 nm
Stage 1
CxB(O2C2(CF3)4)2
Blue: obs
Pink: calc
Unexpected anion orientation - long axis to sheets
T

## Slide 22
GIC with alkylammonium cations
1D electron density maps of the flattened bilayer vs. expanded monolayer of (C7H15)4N-GIC.
Small R4N-intercalates; flattened monolayer
Large R4N-intercalates; flattened bilayer
e.g. C41[(C4H9)4N]
e.g. C63[(C7H15)4N]