Measurements of misfit layer compounds thin films

Dmytro Khvostenko

J. Tate Lab, Department of Physics, Oregon State University

8 May, 2009

Samples were supplied by Qiyin Lin (D. Johnson group, University of Oregon). Measurements were performed by Dmytro Khvostenko (J. Tate group, Oregon State University).

- Hall effect and resistivity

Room temperature Hall and resistivity measurements were performed on thin films of the misfit layer compounds (PbSe)x(WSe2)y using a Lakeshore model 7504 Hall effect system. Samples were supplied with In/Au contacts and annealed under desk lamp.  IV curves for all samples were linear. No data was obtained for sample (1:8) due its extremely high resistivity. All the other samples indicate p-type conductivity (the Hall coefficient is positive).

| (PbSe) : (WSe2) | d, A | N, 1/cm3 | μ, cm2/Vs | ρ (ohm cm) |
| --- | --- | --- | --- | --- |
| 1:6 | 646 | 9.6E+19 | 0.0509 | 1.30 |
| 1:2 | 692 | 1.7E+19 | 1.895 | 0.19 |
| 2:1 | 640 | 9.5E+17 | 5.8 | 1.22 |
| 3:1 | 498 | 4.09E+17 | 12.2 | 1.26 |
| 6:1 | 952 | 2.5E+17 | 4.0 | 6.34 |

Table 1.  Transport properties measured from thin films.

The resistivity of the thin films does not have strictly monotonic behavior with respect to the PbSe:WSe2 ratio (Fig. 1), and sample (6:1) shows significantly higher resistivity (6.335 ohm cm) than the other samples. There is, however, and approximate upward trend in resistivity with increase of PbSe, because the resistivity of PbSe is higher than that of  WSe2.

As the ratio (x:y) increases, the carrier concentration monotonically decreases (Fig. 2).

Fig 1. 290K resistivity of (PbSe)x(WeSe2)y. 	Fig 2. 290K carrier density of (PbSe)x(WeSe2)y.

The mobility is “nicely” proportional to ratio (x:y), except for sample (6:1), where the measurement was noisy  due to high resistivity, so the measurement error measurement is quite large  (Fig. 3).

Fig 3.  290K mobility of (PbSe)x(WeSe2)y.	Fig 4.  290K S of (PbSe)x(WeSe2)y.

2. Seebeck measurements.

Fig. 4 represents the dependence of S on (x:y) for T ≈ 291 K. This graph was plotted to see whether Seebeck measurements are consistent with room-temperature Hall and resistivity measurements. Indeed, the results are consistent as expected: samples that have higher mobility have higher Seebeck coefficient. Samples that have higher carrier concentration have lower Seebeck coefficient.

T-dependent Seebeck measurements were carried out on all samples. The minimum attainable temperature depended on the sample resistivity, but overall, the minimum was 150 K.  Below 150 K, the noise level of noise was unacceptably high.

Measurements were performed in closed cycle refrigerator under vacuum.  The Seebeck measurement system is home-built and consists of two Cu blocks against the sample is pressed in thermal and electrical contact.  One block is heated about 5K above the other and the voltage and temperature difference are monitored as the system returns to equilibrium.  The whole system is at a base temperature that can be changed, and we measured the coefficient every 10-20K.  The results are shown in Table 2 and Fig. 5.

| (x:y)=6:1 |  |  | (x:y)=2:1 |  |  | (x:y)=1:2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| T | S (μ V/K) | error | T, K | S (μ V/K) | error | T, K | S (μ V/K) | error |
| 290 | 232 | 2,74 | 291 | 153,44 | 2,899 | 291 | 37,35 | 0,25 |
| 270 | 222 | 11 | 273 | 110,56 | 1,85 | 271 | 35,54 | 0,22 |
| 250 | 213 | 22 | 251 | 111 | 1,7 | 251 | 31,51 | 0,28 |
| 230 | 197 | 35 | 231 | 99 | 3,77 | 231 | 28,73 | 0,21 |
| 200 | 175 | 67 |  |  |  | 216 | 26,19 | 0,27 |
| 190 | 292 | 18,45 |  |  |  | 200 | 23,16 | 0,34 |
| 180 | 310 | 21,2 |  |  |  | 181 | 19,41 | 0,29 |
| 170 | 441 | 29 |  |  |  | 161 | 15,7 | 0,67 |

| (x:y)=1:6 |  |  | (x:y)=3;1 |  |  | (x:y)=1:8 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| T, K | S (μ V/K) | error | T, K | S (μ V/K) | error | T, K | S (μ V/K) | error |
| 170 | 14,45 | 5,65 | 294 | 186,4 | 1,64 | 290 | 5,5 | 0,2 |
| 200 | 17,89 | 3,31 | 271 | 178,15 | 0,88 |  |  |  |
| 230 | 18,72 | 2,03 | 251 | 175,5 | 0,94 |  |  |  |
| 240 | 19,885 | 2,02 | 226 | 169,12 | 1,32 |  |  |  |
| 250 | 19,584 | 1,34 | 201 | 163,99 | 1,76 |  |  |  |
| 270 | 20,324 | 1,04 | 171 | 151,9 | 3,3 |  |  |  |
| 290 | 21,781 | 0,76 | 151 | 126,58 | 4,7 |  |  |  |

Table 2. T-dependence of Seebeck coefficient of (PbSe)x(WeSe2)y.

Fig 5.  Temperature dependence of the Seebeck coefficients of (PbSe)x(WeSe2)y.  The curves are labeled with the x:y ratio.

Fig. 5 shows that the Seebeck coefficient increases as  (x:y) increases for all temperatures.  All samples except 6:1 show metallic behavior, because S(T) is linear (Fig 5). As for sample (6:1), rapid non-linear dependence of S(T) with decreasing temperature below 190K is indicative of semiconducting behavior and may indicate the onset of a metal-insulator trnsition.  Another reason for a large increase in S(T) at low temperature can be phonon drag. This question needs further investigation.  As an aside, we note that we have observed similar increases at low temperature in CuScO2+y for values of y such that the material becomes conducting.  CuScO2 is an insulator that can be made p-type conducting upon O intercalation (y up to 0.5).  For the most conductive samples, a pseudo-metallic behavior is seen at high temperatures, and a strong upturn at low temperatures.

The errors estimates were obtained using the regression tool in the  “Data Analysis” packet in Excel. Errors strongly depend on the sample resistivity (compare Fig. 1 and Fig 5).

Effect of ambient atmosphere:

Seebeck coefficients measured below room temperature are always measured in vacuum, but sometimes room-temperature coefficients are measured at ambient pressure.  There is an interesting difference between the coefficients measured in air (much higher) and in vacuum (lower). Diagram 1 represents Seebeck coefficient for sample (1:2), measured at room temeprature at ambient pressure: S = 52.63 μV/K.   Diagram 2 shows the same measurement at the same T, measured in vacuum – S = 37,39 μV/K, a 30% difference !  The effect is reversible.

Diagram 2

We investigated the effect as a function of pressure 1 atm > P > ≈10-5 torr.  Unfortunately, the gauging on our Seebeck chamber is not optimal and we cannot be exactly certain of the pressure. But we can make a reasonable guess using the duration that chamber is pumped. Diagram 3 represents the Seebeck coefficient 7 min after roughing pump turned on: S = 47.62 μV/K.

Diagram 4 shows S under relatively high vacuum (TMP operational). S = 43.88 μV/K.

It seems that S depends on the pressure at the surface. A rapid change in S occurs during first few minutes of pumping, corresponding to a large pressure change.

We speculate that the effect may be due to water adsorption on the surface which may change the surface conductivity.  As it is reversible, it is unlikely to be due to Se desorption.  In any event, it seems to lend credence to the notion that the Seebeck effect is influenced heavily by the surface.