Substrate Cleaning Procedure

Eric Sundholm

February 13, 2009

Cleaning (Initial)

Glass Substrates (ITO Coated)

- Scribe backside

- Rinse: 18.2 M DI water

- Ultrasonic bath: Contrad 70, 60 min, 45 C

- Rinse: 18.2 M DI water

Note: if Contrad 70 dries to substrate then it is very difficult to remove

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C

Silicon Substrates (SiO2 Coated) – With Scribe

- Scribe

- Rinse: 18.2 M DI water

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C

Silicon Substrates (SiO2 Coated) – No Scribe

- Rinse: IPA

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C

Silicon Substrates (SiO2 Coated) – Chemistry Spin Coating Dielectric

- Scribe

- Rinse: 18.2 M DI water

- Ultrasonic bath: Contrad 70, 60 min, 45 C

- Rinse: copious 18.2 M DI water (if Contrad 70 dries to substrate then it is very difficult to remove)

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C

- Plasma Ash: RIE, 10 min, 200 W, 750 mTorr, 100 sccms O2

Note: this recipe can be found on the RIE as C:\sysmon\process\etches\ash\kaiash

Silicon Substrates (SiO2 Coated) – Chemistry Spin Coating Channel

- Scribe

- Rinse: 18.2 M DI water

- Ultrasonic bath: Contrad 70, 60 min, 45 C

- Rinse: copious 18.2 M DI water (if Contrad 70 dries to substrate then it is very difficult to remove)

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C

Silicon Substrates (Bare) – Chemistry Spin Coating Dielectric

- Scribe

- Rinse: 18.2 M DI water

- Ultrasonic bath: Contrad 70, 60 min, 45 C

- Rinse: copious 18.2 M DI water (if Contrad 70 dries to substrate then it is very difficult to remove)

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C

- Ash: 10 min, O2 plasma, recipe “Kai ash” on RIE

Cleaning (Post Photo / Etch)

Standard Clean

- Remove photoresist: Acetone

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C

Aggressive Clean

- Remove photoresist: Soak, 1165 photoresist stripper, 30 min

- Ultrasonic bath: 1165 photoresist stripper, 5 min

- Rinse: 18.2 M DI water

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C

Lift-off (Post Material Deposition)

Standard Lift-off

- Soak: Acetone, 1 hour

- Ultrasonic bath: Acetone, ~ 2 – 3 min

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 30 min, ~125 C

Note: longer times have been seen to have negative effects on Al contacts (edge pealing, roughening, etc…)

Methane Polymer Build Up Clean (Post ZTO Dry Etch)

Standard Clean

- Plasma ash: RIE, 3 – 4 min, 100 W, 100 mTorr, 2/1/25 (sccms) Ar/CHF3/O2

Note: Can be included with ZTO dry etch recipe without breaking vacuum. Full ZTO (50nm) etch plus polymer clean recipe can be found on RIE as C:\sysmon\process\etches\ZTO\50nmzto

- Remove photoresist / polymer build up: Soak, 1165 photoresist stripper, 30 min

- Ultrasonic bath: 1165 photoresist stripper, 5 min

- Rinse: 18.2 M DI water

- AMD

  - Rinse: Acetone

  - Rinse: IPA

  - Rinse: 18.2 M DI water

- Dry: N2 blow gun

- Dehydrate: Oven, 15 min, ~125 C